## Slide 1: Rammed Earth Blocks
Research for Oxfam

## Slide 2
CINVA RAM and MAKIGA RAM

## Slide 3
Rekindle old technology for 21st century
Test the Makiga ram
Test CINVA ram
Application in transitional settlement
Aim of Research Project

## Slide 4
Produce a block that is cheaper and easier to produce than concrete blocks or fired bricks
A block that is environmentally sound and durable
Use of minimal stabilisation (lime or cement)
Objectives

## Slide 5
Well and latrine liners
Superstructure to latrines
Water tanks
Walls to shelters
Floors
Dwarf walls to tents
Clinics,hospitals, stores, etc
Uses

## Slide 6: Compressive strength is not an issue with rammed earth blocks. Weaker hand moulded blocks reach strengths of 2-4 N/mm2 Durability is an issue. Stabilisation with cement or lime will significantly improve durability

## Slide 12
Two types used in testing:
Clay pit with 40% clay with 50% fine sand and silt. (add 25% 6mm gravel and sand)
A source taken from a metre deep trench, with 20% clay and well graded from fine particle to gravel. (use as dug, removing stones < 10mm)
TROPICAL LATERITIC SOILS?
Earth Samples

## Slide 13
1:20 5% cement
1:12 8% lime
These are minimal. Typical recommended figures suggest 12 – 18%
(concrete would be better in such conditions?)
Stabilisation

## Slide 15: gordon.browne@solent.ac.uk